## Slide 1: The Manufacturing Process ECE4140/6240
Class 2
M. E. Zaghloul
Fall 23

## Slide 2: Integrated Circuits Fabrication The Wafer
Single die
Wafer
Going up to 12” (30cm)

## Slide 3: Die Cost Is Going Down
Single die
Wafer
From http://www.amd.com
Going up to 12”

## Slide 4: Cost per Transistor
0.0000001
0.000001
0.00001
0.0001
0.001
0.01
0.1
1
1982
1985
1988
1991
1994
1997
2000
2003
2006
2009
2012
cost:
¢-per-transistor
Fabrication capital cost per transistor (Moore’s law)

## Slide 5: Yield

## Slide 6: Defects
⍶ is parameter that depends on the complexity
of the fabrication roughly proportional to the number of masks

## Slide 7: STEPS of Fabrications
In the next part we will discuss the most important steps of the fabrication
Please note that the fabrication is done by deposition of materials layer by layer of the different materials used in IC chips-mostly thin film
Thus we should be able to deposit and to etch ( remove) material with the structure we want.

## Slide 8: Quiz
why do we have to understand the fabrication process as CMOS designer?

## Slide 9: For CMOS technology we start from Silicon Wafer Preparation
Obtaining the Sand to grow the wafers has to be very clean and good form of silicon
The Sand is heated to about 1600 degree C where it melt
A pure Silicon seed Crystal is placed into the molten sand bath. This crystal will be pulled slowly while it rotate. The result is called ingot ( single crystal silicon) ( what is crystal?)

## Slide 10: Example of some completed ingots

## Slide 11: Important Steps in IC Silicon Fabrication Processing
Oxidation ( to form the silicon Oxide)
Photolithography to pattern the material
Etching to remove material( thin layer)
Depositions deposit material ( thin layer)
Separate course ECE4145 clean room experience, visit the GWU clean room( at the Basement of the SEH )

## Slide 12: Let us Study each Step
The above listed steps are the basic steps of the clean room fabrication

## Slide 13: Oxidation
Oxidation refer to the process of growing a layer of silicon dioxide onto the wafer surface. This layer is important for two purposes
The silicon oxide is an insulator to electricity. We want to isolate semiconductor transistors to achieve the correct parameters

## Slide 14: Photolithography
It is the selective method for applying thin film materials to the wafer-
First thin film of the desired material is deposited on the whole wafer
Photoresist material is applied on the whole surface of the wafer
Light is shine through a mask then the photoresist is developed and removed Selectively

## Slide 15
Silicon Wafer and
Thin film of material-green
Photoresist is applied-red
Mask you the designer
UV Light

## Slide 16
Develop PR and etch
Patterned thin film

## Slide 17: Etching
Chemical etching is to remove materials selectively from the areas of the wafer
Mostly acid is used to remove thin film selectively

## Slide 18: Deposition
It is the process of depositing a thin film onto the surface of the wafer, the films are Aluminum, or copper, and many other metals.
Most common is the Chemical Vapor Deposition CVD
Low Pressure CVD is done in a vacuum in temp. 300-1250 C. The process deposit high temp oxides, polysilicon, or silicon nitride as thin film with excellent purity

## Slide 19: Ion Implantation
Deposition and diffusion to produce N and P- wells, N+,P+ diffusion
N+, P+ define where areas of thin oxide are needed to implement transistor gate and allow implantation to form p- or n- type diffusion for source /drain

## Slide 20: Cross-Section of CMOS Technology
Side View of Inverter

## Slide 21: CMOS Fabrication Sequence
START P-type wafer bulk
Epitaxial Growth p-epi is used as base layer for building the devices
n-Well Formation the p-channel PMOS must reside in n-type background usually biased at Vdd to insure proper operation
P-epi
P+type

## Slide 22: CMOS Fab (cont.)
n-well for PMOS transistor for the proper biasing
p-substrate
n-well
PMOS
NMOS

## Slide 23: CMOS Fabrication (cont.)
Active area and Isolation , active area is a planar section of the surface where transistors are placed. Isolation regions surround the active areas and constitute the majority of the surface it is called Field Oxide
Interconnect lines such as polysilicon or metals are routed over the Isolations regions allowing us to route transistors and have circuits.

## Slide 24: CMOS Process

## Slide 25: Modern CMOS Process
n-well, p-well, twin-well process, several wells process
Several layers of metals, Al, Cu, and many other metals
Metal contacts are called Via ( metal to metal)
Silicon oxide is an insulator
Metals wirings are called interconnect

## Slide 26: A Modern CMOS Process
Dual-Well Trench-Isolated CMOS Process

## Slide 27: Circuit Under Design

## Slide 28: Well and Substrate Taps
Substrate must be tied to GND and n-well to VDD . Substrate must be biased ( connected to the right voltage) and wells must be biased.
Metal to lightly-doped semiconductor forms poor connection called Schottky Diode
Use heavily doped well and substrate contacts / taps
Remember for invertor the source of the n-transistor is connected to ground and the source of the p-type transistor is connected to VDD

## Slide 29: Inverter Mask Set
Transistors and wires are defined by masks
Cross-section taken along dashed line

## Slide 30: Detailed Mask Views
Six masks
  n-well
  Polysilicon
  n+ diffusion
  p+ diffusion
  Contact
  Metal

## Slide 31: Example-Inverter Fabrication Steps
Start with blank wafer
Build inverter from the bottom up
First step will be to form the n-well
  Cover wafer with protective layer of SiO2 (oxide)
  Remove layer where n-well should be built
  Implant or diffuse n dopants into exposed wafer
  Strip off SiO2

## Slide 32: To cover with thin layer of Silicon Oxide (Oxidation)
Grow SiO2 on top of Si wafer
  900 – 1200 C with H2O or O2 in oxidation furnace

## Slide 33: Photoresist
Spin on photoresist
  Photoresist is a light-sensitive organic polymer
  Softens where exposed to light

## Slide 34: Lithography
Expose photoresist through n-well mask
Strip off exposed photoresist

## Slide 35: Etch
Etch oxide with hydrofluoric acid (HF)
Only attacks oxide where resist has been exposed

## Slide 36: Strip Photoresist
Strip off remaining photoresist
  Use mixture of acids called piranha etch
Necessary so resist doesn't’t melt in next step

## Slide 37: n-Well
n-well is formed with diffusion or ion implantation
Diffusion
  Place wafer in furnace with arsenic gas
  Heat until atoms diffuse into exposed Si
Ion Implantation
  Blast wafer with beam of ions
  Ions blocked by SiO2, only enter exposed Si

## Slide 38: Strip Oxide
Strip off the remaining oxide using HF acid
Back to bare wafer with n-well
Subsequent steps involve similar series of steps

## Slide 39: Polysilicon
Deposit very thin layer of gate oxide
  < 20 Å (6-7 atomic layers)
Chemical Vapor Deposition (CVD) of silicon layer
  Place wafer in furnace with Silane gas (SiH4)
  Forms many small crystals called polysilicon
  Heavily doped to be good conductor

## Slide 40: Polysilicon Patterning
Use same lithography process to pattern polysilicon

## Slide 41: Self-Aligned Process
Use oxide and masking to expose where n+ dopants should be diffused or implanted
N-diffusion forms nMOS source, drain, and n-well contact

## Slide 42: n-Diffusion
Pattern oxide and form n+ regions
Self-aligned process where gate blocks diffusion
Polysilicon is better than metal for self-aligned gates because it doesn't’t melt during later processing

## Slide 43: n-Diffusion (cont’d.)
Historically dopants were diffused
Usually ion implantation today
But regions are still called diffusion

## Slide 44: n-Diffusion (cont’d.)
Strip off oxide to complete patterning step

## Slide 45: p-Diffusion
Similar set of steps form p+ diffusion regions for pMOS source and drain and substrate contact

## Slide 46: Contacts
Now we need to wire together the devices
Cover chip with thick field oxide
Etch oxide where contact cuts are needed

## Slide 47: Metallization
Sputter on aluminum over whole wafer
Pattern to remove excess metal, leaving wires

## Slide 48: CMOS Process at a Glance
Define active areas
Etch and fill trenches
Implant well regions
Deposit and pattern
polysilicon layer
Implant source and drain
regions and substrate contacts
Create contact and via windows
Deposit and pattern metal layers

## Slide 49: Layout
Chips are specified with set of masks designed by the Engineers of IC knowledge
Minimum dimensions of masks determine transistor size (and hence speed, cost, and power)
Feature size f = distance between source and drain
  Set by minimum width of polysilicon
Feature size improves 30% every 3 years or so till today?
Normalize for feature size when describing design rules
Express rules in terms of l = f/2
  E.g. l = 0.3 μm in 0.6 μm process

## Slide 50: Layout Design Rules
λ parameter is popular scalable design rule generally half the minimum width of the polysilicon wire
Lambda based design rules are very conservative
It makes scaling simple
Lambda is half the feature size
Beyond 180nm design rules are more complicated

## Slide 51: Simplified Design Rules Basic CMOS design
Conservative rules to get you started

## Slide 52: Its Layout View

## Slide 53: Advanced Metallization

## Slide 54: 3D Perspective
Polysilicon
Aluminum

## Slide 55: CMOS Process Layers
Layer
Polysilicon
Metal1
Metal2
Contact To Poly
Contact To Diffusion
Via
Well (p,n)
Active Area (n+,p+)
Color
Representation
Yellow
Green
Red
Blue
Magenta
Black
Black
Black
Select (p+,n+)
Green

## Slide 56: Layers in 0.25 mm CMOS process

## Slide 57: Design Rules
Interface between designer and process engineer
Guidelines for constructing process masks
Unit dimension: Minimum line width
  scalable design rules: lambda parameter
  absolute dimensions (micron rules)

## Slide 58: Intra-Layer Design Rules
Metal2
4
3

## Slide 59: Transistor Layout
Poly
N-diffusion

## Slide 60: Vias and Contacts Metal blue, Purple

## Slide 61: CMOS Inverter Layout

## Slide 62: Layout Editor

## Slide 63: Design Rule Checker built in CADENCE
poly_not_fet to all_diff minimum spacing = 0.14 um.

## Slide 64: Circuit Layout

## Slide 65: Circuit Under Design
This two-inverter circuit (of Figure 3.25 in the text) will be
manufactured in a twin-well process.

## Slide 66: CMOS INVERTER

## Slide 67: Rules for layout
Every well should have at least one tap
All substrate and well taps should connect directly to the appropriate power supply in metal
Taps should be placed every 5-10 transistors in the wells and on substrate
Place well taps adjacent to the power supply VDD, VGND
NMOS transistors should cluster together near GND line, PMOS transistors should cluster together near VDD
You always design as if you have double wells

## Slide 69: Well Spacing

## Slide 70: 3-INPUT NAND

## Slide 71: Area Estimation

## Slide 72: WIRING tRACK

## Slide 73: Latch up of the chip page 253 Weste-harris
Short of the chip between VDD and VGND
Occurs when parasitic bipolar transistors formed by the substrate causing low resistance path
In addition to the expected nmos, pmos transistors a bipolar transistors result.
To avoid latch up minimize Resub, and Rwell
Process solution

## Slide 74: Latch up

## Slide 75: Sticks Diagram We will show examples
Dimensionless layout entities
Only topology is important
Final layout generated by “compaction” program

## Slide 76: Summary
CMOS N-well, P-well, dual wells
Well contacts are P+ for P-well (or P-substrate), and N+ for N-well
Contacts metal to p-active, metal to n-active, metal to poly, or metal to well or substrate
Via is contact between metal layers
Well contact to the right voltage is extend to surround the well and called well guard

## Slide 77: Summary
SCMOS means scalable CMOS design rules.
Lambda based design rules in the old technology
Simple and freely available, and easily migrate from one process to another
MOSIS –SCMOS rule are Lambda based

## Slide 78: Summary
Technology for this class by On ( semiconductor company) 0.5 um, N-Well technology
3-metal layers, 1-2 poly layers
Lambda = 0.35micron
MOSIS rules SCMOS scale for
Lambda =1.0-------2 micron
Lambda = 0.8-----1.5 micron
Lambda = 0.35----0.5 micron

## Slide 79: For the Dies connection Bonding Techniques

## Slide 80: Package Types

## Slide 81: Package Parameters

## Slide 82: Summary of Today Class
Fabrication steps for CMOS
CMOS layers and Design Rules
Scalable CMOS – Design Rules in chip design
Introduction to IC layout